## Slide 1
Unit 11.
Eco-informed material selection
Mike Ashby
Department of Engineering,
University of Cambridge
Notes: The PowerPoint Lecture Units For 2024
The Lecture Units developed for teaching in connection with Ansys Granta EduPack are listed at the end of this presentation.

## Slide 2: Learning objectives for this lecture unit
Intended Learning Outcomes | 
Knowledge and Understanding | Understanding advanced tools for eco-informed design and material selection
Skills and Abilities | Ability to use trade-off plots and Materials Indices in eco-selection
Values and Attitudes | Appreciation of the possibilities to reduce environmental impact by design
Resources
Text: “Materials and the Environment”, 3rd Edition by M.F. Ashby, Butterworth-Heinemann, Oxford 2021, UK. Chapters 9-10
Text: “Materials: engineering, science, processing and design”, 4th Edition by M.F. Ashby, H.R. Shercliff and D. Cebon, Butterworth Heinemann, Oxford 2019, Chapter 20
Text: “Materials Selection in Mechanical Design”, 5th Edition by M.F. Ashby, Butterworth Heinemann, Oxford, 2016. Chapter 14
White Paper: Ansys Granta EduPack for Eco Design
Software: Ansys Granta EduPack with Eco Audit tool
Poster: Eco Design
Notes: Learning Objectives
These Intended Learning Outcomes are based on a taxonomy of knowledge and understanding as the basis, skills and abilities as necessary for the practical use of knowledge and understanding, followed by acquired values and attitudes enabling assessments and responsible use of these abilities.
Combined with a suitable assessment, they should be helpful in the context of accreditations or for the CDIO Syllabus.
The Texts listed are from books authored or co-authored by Mike Ashby but other texts are also referred to in the Science Notes.

## Slide 3: Outline of Lecture Unit 11
Eco-informed selection – the strategy
Case study: drink containers
Case study: crash barriers
Notes: Outline
This is the eleventh Unit of a course on Material and Process Selection. The Units link closely to the first three Texts listed on the previous frame but can equally by used in conjunction with texts such as Callister, Budinski, Askeland and others. The relevant chapters of the Texts are listed on the Outline frame of each Unit. The methods developed in the course are implemented in the Granta EduPack software, which is structured to evolve in pace with the student throughout a four-year engineering program. This first Unit introduces materials and processes, and the way in which information about them can be classified, stored, retrieved and explored.

## Slide 4: Eco-informed design
The materials life-cycle
The drivers for eco-design
  Focus on carbon footprint by governments
  Legislation (Carbon taxes, EuP, REACH)
  Incentives (Subsidies, concessions)
  Urge for “responsible” manufacture
  Doing more with less = $$$
Eco-informed design
  80% of eco-impact tied in at design stage
  Build-in eco criteria at the design stage
Notes: The need for eco-informed decisions early in the design process
It is estimated that 80% of the final eco-demands (and the cost) of a product are built in at the design stage. Many governments have committed their nations to reducing green-house gas emissions and interpret this as reducing the release of carbon to the atmosphere. In Europe the Energy-using Products (EuP) Directive requires an eco-analysis of products and a demonstration that the designers have considered the use of energy in their product as it relates to materials, manufacture, packaging transport and distribution, use, and end of life. Registration, Evaluation, Authorization and Restriction of Chemical Substances (REACH) Directive places responsibility on manufacturers to manage risks from chemicals and to find substitutes for those that are most dangerous. Carbon taxes, subsidies for low-carbon emitting products and other incentives all exert pressure to improve eco-design.
The Granta EduPack Materials and Sustainable Development database contains a data-table of Legislation and Regulations (See Lecture Unit What is a Sustainable Development).

## Slide 5: Eco-informed selection: the strategy
Use Eco Audit or other tools
to identify design objective
The steps
Explore options with “What if...”s
Analyse results,
Identify priorities
Fast
Eco Audit
Use EduPack to select
new Materials
and/or Processes
Recommend
actions & assess
potential savings
600
400
300
200
100
0
-100
Material
Manufacture
Transport
Use
Disposal
EoL credit
Initial and re-design
Energy (MJ)
When we did “what if’s” we were guessing
Can we do better? Be systematic?
Apply the selection methodology
Click on bar for advice
Notes: Responding to the Eco Audit
A systematic analysis of materials selection, targeting the most energy and carbon-intensive phases of life, starts with the output of the eco-audit. The eco-audit identifies the design objective that is a key input for the established materials selection methodology that is built into the Granta EduPack software.

## Slide 6: Eco-selection for a fizzy drink bottle
Material Manufacture Transport Use
End of life
400
300
200
100
0
-100
-200
Energy (MJ)
100% virgin PET
with recycling
Eco Audit
Improve green credentials of bottle
Design brief
Translation
Constraints
  Able to be molded
  Transparent / translucent
  Able to contain pressure
  Objectives
  Minimize embodied energy of bottle
  Minimize material cost of bottle
Material
dominates
Minimize embodied energy
Notes: A pressurized drink bottle (a mini pressure vessel)
Here is an example: systematic selection for the carbonated drink bottle. In its present form it is made of polyethylene terephthalate, PET. The audit shows that the material-energy of the bottle itself is the phase of life that consumes the most energy and releases the most carbon. The design brief is to improve the eco-profile of the bottle, which must at the same time be transparent (or at least translucent) so that the contents are visible, and the bottle must withstand the internal pressure and any accidental overloads without yield or bursting. The objective is to minimize the embodied energy per bottle.

## Slide 7: Modelling the bottle
Cylindrical pressure vessel
Circumferential stress
Find material with lowest energy, seek largest
Embodied energy per unit area of wall
Find material with lowest cost, seek largest
Price / kg of material
Embodied energy / kg of material
R= Bottle radius
t = Thickness of bottle wall
p = Internal pressure
σy = Yield strength of material
ρ = Density of material
Hm = Embodied energy of material/kg
E = Embodied energy/m2 of wall
Cm = Material cost per kg
Notes: Modelling to identify the material indices
The bottle is modelled as a cylindrical pressure vessel. The internal pressure p creates a stress in the wall of the bottle, as indicated in the diagram. The circumferential stress is the larger one – its value is listed at the top. This stress must not exceed the yield strength of the material of the bottle, setting a minimum value for the wall thickness, t.
The embodied energy E of the bottle per unit area of wall is given by the second expression. The pressure p and the bottle radius R are fixed by the design. The energy E is minimized by seeking materials with the lowest value of the material property group Hmρ/σy, or the maximum value of its reciprocal. The quantity is the material index for the problem.

## Slide 8: Selection to minimize embodied energy
Bio-polymers are colored green
PLA meets the constraints at lowest embodied energy
First apply constraints, then use index to optimize choice
Increasing
  Further Constraints to Apply
  Able to be molded
  Transparent / optical quality
1
Notes: Choice to minimize embodied energy
This is a chart of yield strength vs. embodied energy per unit volume for polymers that are translucent or transparent. The contours show the index from the previous frame. Biopolymers are shown in green to distinguish them from those that are derived from oil, shown in blue. Two of these – polylactide, PLA and polyhydroxyalkanoates (PHA) perform exceptionally well. PLA, in particular, offers a reduction of embodied energy per bottle of about 40%.

## Slide 9: Selection to minimize cost
PET meets the constraints at lowest cost
Bio-polymers are colored green
Increasing
Can’t ignore cost
1
Notes: Choice to minimize cost
Why, then, are so few bottles made of PLA? Here is a chart of yield strength vs. cost per unit volume for the bottle. The contours show the material cost per unit area of bottle wall. By this criterion the bio-polymers (green) do not do so well. The cheapest material is PET – the material of choice for almost all pressurized drink bottles…

## Slide 10: Trade-off plot
Bio-polymers are colored green
Minimizing both embodied energy and cost
Exchange constant cost/energy not established
Notes: The trade-off between embodied energy and cost
This is a plot of the embodied energy index against the cost index – we wish to minimize both. The trade-off surface is sketched. The materials nearest to the surface are the best choices: PET and PLA.
To distinguish between them we need a penalty function, which requires a value for the exchange constant linking cost and embodied energy (the value of saving embodied energy or carbon) – and thus far there is no agreement on this value. This highlights a difficulty in reaching unambiguous selection for eco-problems: the value of the environment is a matter for debate.

## Slide 11: Materials for crash barriers
Static barrier
Mobile barrier
Bending strength
per unit mass
Criterion:
Bending strength
per unit embodied energy
Function: Absorb impact, transmit load to energy-absorbing units or supports
Index:
Material
dominates
M Mf Tr Use
Dominant
phase of life:
Energy
M Mf Tr Use
Use
dominates
Minimize embodied energy
Minimize mass
Notes: Case Study: Crash barriers
Barriers to protect driver and passengers of road vehicles are of two types: those that are static – the central divider of a freeway, for instance – and those that move – the fender of the vehicle itself (this frame). The static type line tens of thousands of miles of road. Once in place they consume no energy, create no CO2 and last a long time. The dominant phases of their life in the sense of Frame 4 are those of material production and manufacture. The fender, by contrast, is part of the vehicle; it adds to its weight and thus to its fuel consumption. The dominant phase here is that of use. This means that, if eco-design is the objective, the criteria for selecting materials for the two sorts of barrier will differ.
This frame shows the two types of barrier and a schematic eco-audit for each. For the static barrier on the left it is the material phase of life that is dominant, making the reduction of material energy the objective in redesign. For the mobile barrier on the right it is the contribution of the barrier mass to the mass of the vehicle that, over life, results in the largest commitment of energy, making a reduction in mass the objective in redesign.
In use (that is, in a crash situation) the barriers are loaded in bending – they must be strong enough in bending to transmit the load to the supports of the road barrier or to the energy-absorbing crush units on the car. The bottom line shows the relevant index. That for the static barrier on the left characterizes materials with low embodied energy per unit bending strength; that on the right characterizes low mass per unit bending strength. Both are plotted on the frames that follow.

## Slide 12: Static barrier: the index as bar chart
Selected materials: Steels, Cast irons
Metal Polymers Composites
Notes: Plot of the index for the static barrier
The Y-axis of this chart is the index for the static barrier, made with Granta EduPack Level 2. The green selection box isolates the materials with the largest values of this index. They are all ferrous alloys – steels and cast irons. They minimize the life-energy of a static barrier by minimizing the most energy-intensive phase – that of material extraction, casting and rolling.

## Slide 13: Mobile barrier: the index as bar chart
Metal Polymers Composites
Selected materials: CFRP, Mg alloys, Ti alloys, Al alloys
Notes: Plot of the index for the mobile barrier
The Y-axis of this chart is the index for the mobile barrier, again made with Granta EduPack Level 2. The green selection box isolates the materials with the largest values of this index: CFRP and light alloys. They minimize the life-energy of a mobile barrier by minimizing the most energy-intensive phase – that of product use.

## Slide 14: Summary
Systematic strategies, using material indices, optimize material choice to minimize life energy
Granta EduPack allows the strategy to be implemented and documents the steps taken to minimize eco-impact.
Eco-informed material choice is part of the eco-design process
An Eco Audit identifies the most damaging phase of life and identifies strategies for overcoming it
Notes: Summary
This final frame summarizes the main findings of this Unit.

## Slide 15: Lecture unit series
PowerPoint lecture units, as well as many other types of resources, can be found in the Ansys Education Resources webpage.
www.ansys.com/education-resources
Finding and Displaying Information | 
Unit 1 | The materials of engineering
Unit 2 | Material property charts: mapping materials
Unit 3 | The Elements database: properties, relationships and resources
Material Properties | 
Unit 4 | Manipulating properties: composition, microstructure, architecture
Unit 5 | Designing new materials: filling the materials-property space
Unit 6 | Materials Science and Engineering
Selection | 
Unit 7 | Material selection: translation, screening, ranking, documentation
Unit 8 | Objectives in conflict: trade off methods and penalty functions
Unit 9 | Material and shape: materials for efficient structures
Unit 10 | Manufacturing processes and cost modeling
Unit 11 | Eco-informed material selection
Unit 12 | Eco design and the Eco Audit tool
Sustainability
What is a sustainable development? A materials perspective
Exploring Critical Materials using Ansys Granta EduPack
Special Topics
The Built Environment: materials for construction
Structural sections: shape in action
Materials in industrial design: Why do consumers buy products?
The Design database for Products
The Medical Devices database
The Battery Designer tool
Advanced Teaching and Research
Advanced databases: a lightning tour
The Aerospace edition
The Polymer edition
The Synthesizer tool: hybrids and other models
Materials for Bioengineering
Notes: Lecture Units Series
This is a list of the Lecture Units available for teaching with the Ansys Granta EduPack. These PowerPoint presentations and more information can be found on the Ansys Education Resources webpage:
www.ansys.com/education-resources.