## Slide 1
Fundamentals of Crystallography and Crystal Defects Lecture
Kaitlin Tyler, PhD
Ansys Academic Program

## Slide 2: Learning Objectives
Intended Learning Outcomes | 
Knowledge and Understanding | Identify different crystal systems
Skills and Abilities | Label planes and directions in crystal systems using Miller Indices
Values and Attitudes | Understand how crystallinity can affect material properties
Resources
Texts: (1) Callister, W. D. & Rethwisch, D. G. Materials Science and Engineering: An Introduction. (John Wiley & Sons, Inc., 2018)., (2) Porter, D. A., Easterling, K. E., & Sherif, M. (2009). Phase Transformations in Metals and Alloys, (Revised Reprint). CRC press.
Granta EduPack for All Majors- Teaching with Callister Paper
Further reading/information
  Ansys Academic
  Ansys Innovation Courses
  Ansys Education Resources
Ansys software mentioned | Ansys Granta EduPack™ teaching software for materials education

## Slide 3: Outline of this Lecture Unit
Amorphous vs. Crystalline Materials
Crystallinity Fundamentals
  Unit Cells
  Miller Indices
Crystal Defects
  Definition
  One, two, and three-dimensional defects
Notes: This lecture unit focuses on fundamentals of crystallography. Starting by defining what crystalline materials are, we move into the fundamental structure: the unit cell. The impact of knowing the crystal orientation on material performance and how we denote these orientations through Miller Indices will be discussed. Then, we move on to what happens when a material is not a perfect crystal. Defect types are defined and the impacts that defects can have on a system, both positive and negative, are shown.

## Slide 4: Impacts of Atomic Structure
Fused Silica Glass
© Stefan Wernli, stef at en.Wikipedia-(CC BY_SA 2.5) 2.
Quartz
Piezoelectric
  Helps keep time in watches
Chemical composition:
US Geological Survey
Highly resistant to temperature and thermal shock
Chemical composition:
How can these compositions be identical when the products and uses are so different?
Notes: Atomic structure can have a large impact on a materials properties and performance.
An example of this starts with fused silica glass. This material is highly resistant to thermal shock and high temperatures and is almost 100% silica, or Si O 2.
On the other hand, you have quartz. This is the material in watches that helps keep time due to the piezoelectric nature of the material, where mechanical loading causes an electric potential to form. This material is also made from almost 100% silica.
So how do these identical materials behave so differently?

## Slide 5: Crystalline vs. Amorphous
Crystalline Materials:
A solid material characterized by a periodic, repeating, 3D arrangement of atoms, ions, or molecules
Often opaque
Example: Quartz, salt, aluminum
Amorphous Materials:
A solid material that lacks a long-range crystalline order
Often transparent
Example: Glass, some polymers
Notes: The reason is the different in atomic structure between the two cases of Silica. Quartz is a crystalline material, where the atoms are arranged in an ordered, repeating structure. Fused silica, on the other hand, is amorphous. This means the material lacks this long-range order. The difference in atomic order can impact many things about a material, from how it transports heat to how light interacts with the materials.
Question for the class: Can you think of some material properties that crystal structure, and therefore bond arrangement, could impact?

## Slide 6: Unit Cells: the Basics of Crystals
The smallest repeating unit within a crystal
There are seven crystal systems:
Cubic
Rhombohedral
Tetragonal
Hexagonal Close-Packed
All sides are equal
All angles are equal to 90°
All sides are equal
Notes: The building blocks of crystals are called unit cells. These are the smallest repeating units.
There are seven commonly discussed crystal systems. They are separated due the degree of symmetry within the unit cell.
The first is cubic, which has the highest symmetry. There are many variations of cubic, which will be discussed later. It is also one of the most common, with examples such as aluminum, germanium, and copper.
Next is Rhombohedral, which differs due to an angle along one axis not being 90. An example material is bismuth.
Tetragonal materials are elongated along one axis with all angles equaling 90. An example material is Indium
Hexagonal close-packed unit cells are also very common, with an elongation along one axis and one angle equaling 120 degrees. This is the only one of the seven that is not based in a quadrilateral and is based instead in a hexagon. An example material is cobalt

## Slide 7: Unit Cells: the Basics of Crystals
Orthorhombic
Monoclinic
Triclinic
The smallest repeating unit within a crystal
There are seven crystal systems:
Notes: *Continuing information onto another slide for space
These next systems start to break symmetry.
Orthorhombic materials have square angles but no sides equal one another. An example material is uranium
Monoclinic materials have two square angles but no equal sides. An example material is phosphorus
Triclinic has no equal angles or sides. It is a complex structure lacking symmetry. An example material is turquoise.

## Slide 8: Common Unit Cells
Hexagonal Close Packed
Body-Centered Cubic
Face-Centered Cubic
Notes: When discussing unit cells and talking about the fundamentals, three are commonly discussed– Face Centered Cubic, Body Centered Cubic, and Hexagonal Close Packed

## Slide 9: Why do I care about crystal structure?
Alloy design
Hume Rothery Rules
  Atomic size factors
  Crystal structure
  Electronegativity factor
  Valences

## Slide 10: Crystal Symmetry
Each unit cell has a different degree of symmetry.
But why is this important?
Notes: Discussion point within the class– let students give their thoughts and opinions before moving on

## Slide 11: Impact of Crystal Symmetry
Example: Single Crystal with a High Degree of Symmetry Unit Cell
Unit Cell (FCC)
All cube faces are symmetrical
Identical crystal orientation after rotation
Example: Single Crystal with a Low Degree of Symmetry Unit Cell
Unit Cell (Triclinic)
Shape faces are not symmetrical
Different crystal orientation after rotation
Color identical cube faces
Rotate 120°
Color identical cube faces
Rotate 120°
Notes: Different unit cells have vastly different faces, as demonstrated by the schematic on the slide. Question how this might impact properties (mechanical? Thermal?)

## Slide 12: Orientation within a single Unit Cell matters too!
3D Unit Cell
2D cross section
What notation do we use to describe these unit cell orientations?
Notes: Emphasize how, even within a single unit cell, the orientation matters depending on how the cell is rotated. The gray planes highlighted in the 3D unit cells– try to have students visualize this face being the “top” of the unit cell. That dramatically changes the look of the cell and therefore will have an impact on properties. Therefore, we need a way to talk about these planes and directions within unit cells that is uniform across all of materials science. But how do we do this?

## Slide 13: Miller Indices for Directions and Planes
Need a language to describe orientations within cubic crystal systems

## Slide 14: Labeling Directions within Cubic Systems
[011]

## Slide 15: Labeling Planes within Cubic Systems
(102)

## Slide 16: Why does orientation matter?
Anisotropy
When a material exhibits different values for a property depending on the crystallographic direction
Ex: Modulus of Elasticity for Aluminum
Material | Modulus of Elasticity (GPa) |  | 
 | [100] | [110] | [111]
Aluminum | 63.7 | 72.6 | 76.1
Source: R.W.Hertzberg, Deformation and Fracture Mechanics of Engineering Materials, 3rd. Edition. Copyright © 1989 by John Wiley & Sons, New York. From Callister, W. D., & Rethwisch, D. G. (2018). Materials science and engineering : an introduction (10th ed.). Pg. 81. Wiley.

## Slide 17: Close Packed Crystal Systems
Hexagonal Close Packed
Face-Centered Cubic

## Slide 18: Close packed
(111)
(0001)

## Slide 19: Atomic Packing Impacts Material Density

## Slide 20: Single vs. Polycrystalline
Uniform crystal orientations throughout the whole material
Segments of different crystal orientations throughout the whole material

## Slide 21: Why do I care about single crystal?
Jet engine turbine blades are grown as single crystals for improved mechanical properties at extreme high temperatures
Otherwise, the blades would droop!
You can learn more here: Each Blade a Single Crystal | American Scientist

## Slide 22: Crystal Defects
Definition: a Lattice distortion or irregularity within a material
No material is 100% perfectly crystalline!
Defects can be 1-dimension, 2-dimensions, or 3-dimensions

## Slide 23: Point Defects (1-D)
Self-interstitial
Interstitial
Substitutional
Vacancy

## Slide 24: Linear Defects: Dislocations (2-D)
Edge Dislocation b ꓕ to the dislocation line
Screw Dislocation
b // to the dislocation line
Type of dislocation is defined by the orientation and magnitude of the lattice distortion or the Burger’s Vector, b

## Slide 25: Planar Defects (3-D)
Grain Boundaries
Twin Boundaries
Stacking Faults
Extrinsic
Intrinsic

## Slide 26: Defects are always undesirable, right?
Not necessarily!
Example: Hall Petch strengthening

## Slide 27: Conclusion
Materials can exist in a variety of atomic arrangements
  Both crystalline and amorphous
Crystallographic orientation matters and Miller Indices are used to define these orientations
Crystals will always have defects
  These defects can exist in 1, 2, and 3 dimensions
  Defects are not always undesirable

## Slide 28: Ansys Education Resources Feedback Survey
Here at Ansys, we rely on your feedback to ensure the educational content we create is up-to-date and fits your teaching needs.
Please click the link below to fill out a short survey (~7 minutes) to help us continue to support academics around the world utilizing Ansys tools in the classroom.
Feedback Survey Link
Notes: Feedback Survey link for copy-paste method  https://ansys.typeform.com/to/jcattJI5