## Slide 1
Fundamentals of Phase Diagrams Lecture
Kaitlin Tyler, PhD
Ansys Academic Program

## Slide 2: Learning Objectives
Intended Learning Outcomes | 
Knowledge and Understanding | Identifying key aspects and categories of phase diagrams
Skills and Abilities | Calculating alloy phase fractions using the Lever Rule
Values and Attitudes | Understanding how pressure, temperature and composition impact material phases and the impact on performance
Resources
Texts: (1) Callister, W. D. & Rethwisch, D. G. Materials Science and Engineering: An Introduction. (John Wiley & Sons, Inc., 2018)., (2) Porter, D. A., Easterling, K. E., & Sherif, M. (2009). Phase Transformations in Metals and Alloys, (Revised Reprint). CRC press.
Granta EduPack for All Majors- Teaching with Callister Paper
Further reading/information
  Ansys Academic
  Ansys Innovation Courses
  Ansys Education Resources
Ansys software mentioned | Ansys Granta EduPack™ teaching software for materials education

## Slide 3: Understanding phase transformations in different environments
Example: Water
1 atmosphere
Approx. 0.005 atmosphere
Solid phase: ice
Solid phase: ice
Gas phase: water vapor
Liquid phase: water
Gas phase: water vapor
0˚C
100˚C
approx. 0˚C
Notes: Water is a familiar material that has well understood phase transitions at normal atmosphere
What happens when we aren’t at normal atmosphere?
What could this be used for? (ex: super critical drying)

## Slide 4: Phase Diagrams help us understand these impacts
Definition: Phase Diagrams graphically show information about the equilibrium phase structure of a system with respect to temperature, pressure, and composition(s)
https://courses.lumenlearning.com/cheminter/chapter/phase-diagram-for-water/
Notes: Phase diagrams are used in alloy design and understanding across all of materials science. By learning the fundamentals of how these are created, we begin to see how impactful they are.
Equilibrium diagrams– discuss what this means for real life, which is not equilibrium

## Slide 5: What is a phase?
Definition: a homogeneous portion of a system that has uniform physical and chemical characteristics
More than just liquid, solid, and gas!
Alpha Titanium
Stable below 882˚C
HCP Crystal Structure
Beta Titanium
Stable between 882-1670˚C
BCC Crystal Structure
882°C
Notes: You are familiar with phases from your previous science courses and general life experience. But materials can have more than one unique solid or liquid phase– this can dramatically impact material properties and thus its performance. It is important to pay attention to these details, which can be found on phase diagrams.

## Slide 6: What is a component?
Definition: the pure metals and/or compounds that alloys are composed of
  Which terms are plotted for a multi-component system?
Single component phase diagrams show temperature and pressure
One composition held constant
Notes: Discussion of what a component is (not just atoms)
  Can be water, Aluminum, NaCl, etc.
How do we plot four variables (composition of component A, composition of component B, temperature, pressure) in 2D?

## Slide 7: Binary Phase Diagrams
Graphical representation of the phases present for a two-component system
Two axis are temperature (y-axis) and composition (x-axis)
  Third variable pressure, is assumed to be one atmosphere
Most common in materials engineering

## Slide 8: Binary Isomorphous Phase Diagrams
Complete liquid and solid solubility
  Only one liquid and solid phase across the complete composition range
Often due to similar atomic crystal structures of the two components
E.g. Copper and Nickel
Notes: -- Complete solid solubility– how common is this?
* Optional in-class activity: use GRANTA EduPack to find some other metal elements that are similar in crystal structure and atomic size. Then search for a phase diagram (either in EduPack or online). Do they have complete solid solubility?

## Slide 9: Binary Eutectic Phase Diagram
Incomplete solubility within the solid phases
Leads to a eutectic reaction at a specific composition and temperature
  Where the liquid solidifies into two unique solids, alpha and beta
Beta
Microstructure:
Alpha
Notes: Notice the region of non-solubility. Eutectic reactions are not the only type of phase reaction that can occur during solidification– more in a few slides

## Slide 10: Key Phase Diagram Terminology
Notes: There are different terminology associated with phase diagrams that we will go through now

## Slide 11: Key Phase Diagram Terminology
Liquidus
Notes: The temperature at which, for a given composition, solidification begins upon cooling (GRANTA EduPack 2020)

## Slide 12: Key Phase Diagram Terminology
Solidus
Notes: The temperature at which solidification, for a specific composition, ends upon cooling (GRANTA EduPack 2020)

## Slide 13: Key Phase Diagram Terminology
Solvus
Notes: When a solvus line is crossed upon cooling, precipitates of a second phase will form (GRANTA EduPack 2020)
Based on this definition, why is there no solvus line on an isomorphous diagram?

## Slide 14: Solubility within Phases
Solubility in binary eutectic systems varies
Solvus line helps show the solubility of B in the Alpha phase and A in the Beta phase
Low solubility in primary phases
High solubility in primary phases
Notes: How does the degree of solubility of A in B change as the system cools? Why? Is this what you would expect based on personal experience (ex: trying to dissolve sugar into a cup of coffee/tea)?

## Slide 15: Phase Transformations
Definition: where one or more phase within a system change into new phase(s)
Common phase transformation example: ice melting
Phase transformation from solid to liquid
Ice melting and other single component system changes are considered congruent transitions
Congruent transitions: a phase transformation with no compositional change
Reaction visual within a phase diagram
Reaction:
Notes: Why do we care about phase transformations?
Why would this be important for processing?

## Slide 16: Phase Transformations
Eutectic transformation: the composition and temperature at which two liquidus lines meet. The liquid transforms to two intermixed solid phases
Reaction visual within a phase diagram
Reaction:
Eutectoid transformation: one solid phase transforming isothermally and reversibly into two intermixed solid phases
Reaction visual within a phase diagram
Reaction:
Notes: -tic Liquid to solid transformation
-toid solid to solid transformation
Eutec start with one phase, end with two

## Slide 17: Phase Transformations
Peritectic transformation: reaction where a solid and a liquid transform into a solid phase with a different composition
Reaction visual within a phase diagram
Reaction:
Peritectoid transformation: reaction where two solid phases transform reversibly into a solid phase with a different composition
Reaction visual within a phase diagram
Reaction:
Notes: -tic Liquid to solid transformation
-toid solid to solid transformation
Peritec start with two phases, end with one

## Slide 18: Phase Transformations
Monotectic transformation: a liquid phase transforming to a solid phase and a liquid phase of a different composition
Reaction visual within a phase diagram
Reaction:
Notes: Mono two different liquids

## Slide 19: Phase Fractions within Systems
Understanding what phases will be found at specific composition and temperature is incredibly important for alloy development
In a single-phase regions, identifying phase fractions is simple
In two-phase regions, the Lever Rule is needed to calculate the phase fractions

## Slide 20: Lever Rule
Used to calculate various phase and microconstituent fractions for two phase regions of binary phase diagrams
Information needed:
composition and temperature of interest.
e.g.: 20 wt.% B and 50 ˚C

## Slide 21: Lever Rule Steps
Step 1:
Draw a tie line across the two-phase region
Step 2:
Identify points of interest

## Slide 22: Lever Rule Steps
Step 3:
To determine the phase fraction, take the distance from the composition to the other phase divided by the total

## Slide 23: Derivation
Assumptions:
For a two-phase region, the weight fractions must add up to 1
The mass of component B in both phases must add up to the total amount of B in the alloy

## Slide 24: Derivation
α phase
β phase

## Slide 25: What can the Lever Rule Determine?
Weight fraction of single phases
  Liquid, alpha, beta, etc.
Weight fraction of microconstituents
  Eutectic, Pro-eutectic phase alpha or beta, etc.

## Slide 26: Microstructure Evolution
Lead Tin diagram
Path 1
Path 2
As alloys solidify, their microstructure will evolve based on the composition
Phase diagrams can help give insight as to what microstructure will form
Notes: Remember, this is for equilibrium systems– discuss what might happen in non-equilibrium (coring, etc.)

## Slide 27: Conclusion
Phase diagrams are an integral part of materials science and engineering
Understanding what phases are stable in equilibrium for various systems is crucial for design
Phase diagrams can be used to determine phase weight fraction, microstructure evolution, solubility, and a variety of other factors

## Slide 28: Ansys Education Resources Feedback Survey
Here at Ansys, we rely on your feedback to ensure the educational content we create is up-to-date and fits your teaching needs.
Please click the link below to fill out a short survey (~7 minutes) to help us continue to support academics around the world utilizing Ansys tools in the classroom.
Feedback Survey Link
Notes: Feedback Survey link for copy-paste method  https://ansys.typeform.com/to/jcattJI5