## Slide 1
Simulating A Forging Process in Ansys Mechanical software
Authors: Dr. Rajesh Bhaskaran*, Dr. Mostafa Hassani*1 & Dr. János Plocher *2
* Cornell University – Swanson Teaching Professor of Engineering Simulation *1 Cornell University – Assistant Professor jointly within the Sibley School of Mechanical & Aerospace Engineering *2 Ansys (Part of Synopsys ) – Academic Simulation Program Lead

## Slide 2: Learning Objectives
Intended Learning Outcomes | 
Knowledge and Understanding | Manufacturing process simulation including non-linear contacts and material behaviour.
Skills and Abilities | Ability to use the Ansys Mechanical software to set up a non-linear static structural simulation.
Values and Attitudes | Awareness of the importance of simulation in manufacturing and link to analytical solution.​
Resources
  SimCafe Cornell University – Ansys Learning Modules.
  G.E. Dieter: “Mechanical Metallurgy”, 3rd ed., McGraw-Hill, 1986.
Built-in Assessment
Simulation Tutorial
Quiz Question
Further reading/information
  Ansys Academic
  Ansys Innovation Courses
  Ansys Education Resources
Ansys software mentioned | Ansys MechanicalTM structural finite element analysis software
Notes: Learning Objectives

## Slide 3
Problem Statement
Plain Strain Forging
Notes: Problem Statement - Plain Strain Forging

## Slide 4: Plain Strain Forging: Problem Statement
Task:
  Determine the pressure distribution between in the middle of the workpiece for a coefficient of friction between workpiece and die of =0 and =0.1.
  Analyse the forging process in 2D
Given:
  Half the workpiece length:
  Workpiece height:
  Y-displacement top die:
  Workpiece Young’s modulus:
  Workpiece Poisson’s ratio
  Workpiece yield strength:
  Workpiece BISO* tangent modulus:
  Die Young’s modulus (inf. stiff): 𝐸 𝐺𝑃𝑎
  Die Poisson’s ratio: 𝜈
*Bilinear Isotropic Hardening
A:A
Top die
Bottom die
Workpiece
Infinitesimal section
A:A
Notes: Plain Strain Forging: Problem Statement
Context:
Forging is a manufacturing process where metal is shaped by applying compressive forces, typically using hammers, presses, or dies. It improves material properties by refining grain structure and enhancing strength.
Plane strain assumption in forging:
  Only applicable for a long rectangular workpiece where the length >> height, width.
  The center region behaves 2D, i.e. deformation occurs primarily in two dimensions (x and y), while strain in the third direction (z) is negligible.; ends experience 3D flow.
  This assumption simplifies analysis because the material flow is constrained, making it ideal for studying stress distribution and pressure requirements.
The dies apply compressive force on the workpiece, and friction at the die-workpiece interface significantly influences pressure distribution and material flow.
Problem Statement:
We need to determine the pressure along the entire contact surface between the die and the workpiece.
Two cases are considered:
  Frictionless contact (): Idealized scenario for baseline analysis.
  Frictional contact (): More realistic condition, introducing shear stresses and non-uniform pressure.
Tasks:
Calculate pressure distribution for both friction conditions.
Perform a 2D analysis under plane strain assumptions:
  Use equilibrium equations and stress relationships.
  Visualize how friction alters pressure and flow patterns.
Discuss implications for die design and energy requirements.
Plain Strain Forging: Problem Statement
Context:
Forging is a manufacturing process where metal is shaped by applying compressive forces, typically using hammers, presses, or dies. It improves material properties by refining grain structure and enhancing strength.
Plane strain assumption in forging:
  Only applicable for a long rectangular workpiece where the length >> height, width.
  The center region behaves 2D, i.e. deformation occurs primarily in two dimensions (x and y), while strain in the third direction (z) is negligible.; ends experience 3D flow.
  This assumption simplifies analysis because the material flow is constrained, making it ideal for studying stress distribution and pressure requirements.
The dies apply compressive force on the workpiece, and friction at the die-workpiece interface significantly influences pressure distribution and material flow.
Problem Statement:
We need to determine the pressure 𝑃along the entire contact surface between the die and the workpiece.
Two cases are considered:
  Frictionless contact (𝜇=0): Idealized scenario for baseline analysis.
  Frictional contact (𝜇=0.1): More realistic condition, introducing shear stresses and non-uniform pressure.
Tasks:
Calculate pressure distribution for both friction conditions.
Perform a 2D analysis under plane strain assumptions:
  Use equilibrium equations and stress relationships.
  Visualize how friction alters pressure and flow patterns.
Discuss implications for die design and energy requirements.

## Slide 5: Plain Strain Forging: Analytical Solution
Key Assumptions:
  Plane strain compression of a strip between rigid flat dies
  Constant (current) workpiece thickness ℎ
  Small deformation increment
  Uniform stress through thickness
  No barreling
  Rigid–perfectly plastic material, von Mises yield
Governing Relations:
  Yield condition (von Mises, plane strain):
    (1)
  Slab equilibrium (horizontal):
    (2)
  Governing differential equation (substituting yield into equilibrium condition):
    (3)
*Bilinear Isotropic Hardening
Boundary Condition:
  At the free edge 𝑥=𝑎, there is no longitudinal stress, so the pressure equals the plane-strain yield pressure:
    (4)
  Integrating (3) and (4) finally yields:
Notes: Plain Strain Forging: Analytical Solution
This slide shows how the classical exponential pressure distribution in forging is derived using the slab method. The result provides a benchmark for validating FEM contact and plasticity models.
Geometry and Assumptions
We consider plane-strain compression of a strip with half-width and thickness . The dies are rigid and flat, and friction follows Coulomb’s law. The material is rigid–perfectly plastic and obeys von Mises yielding.
The slab method assumes the geometry is fixed during a small deformation increment, so the thickness is treated as constant.
Yield Condition
Under plane strain, the von Mises yield criterion reduces to a simple linear relation between longitudinal stress and die pressure :
This equation is critical—it closes the problem by linking internal stress to contact pressure.
Slab Equilibrium
We isolate a thin vertical slab of width . Horizontal force equilibrium requires the gradient of longitudinal stress to be balanced by friction acting on the top and bottom surfaces:
The factor of 2 accounts for friction on both dies.
Governing Differential Equation
Substituting the yield condition into the equilibrium equation eliminates and yields:
This is a first-order linear differential equation.
Boundary Condition
At the free edge , there is no longitudinal stress, so the pressure equals the plane-strain yield pressure:
Final Solution
Integrating the equation with this boundary condition gives the exponential pressure distribution:
Physical Interpretation
This result shows that friction causes pressure to increase rapidly toward the center of the workpiece. Thinner workpieces and higher friction coefficients lead to much higher forging loads.
This equation is widely used as:
  A first-order forging load estimate
  A benchmark for FEM simulations of metal forming
Plain Strain Forging: Analytical Solution
This slide shows how the classical exponential pressure distribution in forging is derived using the slab method. The result provides a benchmark for validating FEM contact and plasticity models.
Geometry and Assumptions
We consider plane-strain compression of a strip with half-width 𝑎and thickness ℎ. The dies are rigid and flat, and friction follows Coulomb’s law. The material is rigid–perfectly plastic and obeys von Mises yielding.
The slab method assumes the geometry is fixed during a small deformation increment, so the thickness ℎis treated as constant.
Yield Condition
Under plane strain, the von Mises yield criterion reduces to a simple linear relation between longitudinal stress 𝜎_𝑥and die pressure 𝑃:
𝜎_𝑥+𝑃=2/√3 𝜎_0
This equation is critical—it closes the problem by linking internal stress to contact pressure.
Slab Equilibrium
We isolate a thin vertical slab of width 𝑑𝑥. Horizontal force equilibrium requires the gradient of longitudinal stress to be balanced by friction acting on the top and bottom surfaces:
(𝑑𝜎_𝑥)/𝑑𝑥=−2𝜇/ℎ 𝑃
The factor of 2 accounts for friction on both dies.
Governing Differential Equation
Substituting the yield condition into the equilibrium equation eliminates 𝜎_𝑥and yields:
𝑑𝑃/𝑑𝑥=2𝜇/ℎ 𝑃
This is a first-order linear differential equation.
Boundary Condition
At the free edge 𝑥=𝑎, there is no longitudinal stress, so the pressure equals the plane-strain yield pressure:
𝑃(𝑎)=2/√3 𝜎_0
Final Solution
Integrating the equation with this boundary condition gives the exponential pressure distribution:
𝑃(𝑥)=2/√3 𝜎_0 exp⁡" " [2𝜇/ℎ (𝑎−𝑥)]
Physical Interpretation
This result shows that friction causes pressure to increase rapidly toward the center of the workpiece. Thinner workpieces and higher friction coefficients lead to much higher forging loads.
This equation is widely used as:
  A first-order forging load estimate
  A benchmark for FEM simulations of metal forming

## Slide 6
Theoretical Background and Simulation Setup
Plain Strain Forging
Physical Problem
Numerical Model
Physical Prototype
Final Product
Notes: Theoretical Background and Simulation Setup - Plain Strain Forging

## Slide 7: Material Properties & Quarter Symmetry Model
Bilinear Isotropic Hardening
  Very small, non-zero tangent modulus to improve the numerical stability
Exploiting Symmetry
  Only a quarter of the model is required, due to two symmetry planes, which reduces the computational effort significantly
Notes: Material Properties & Quarter Symmetry Model
For the workpiece a bilinear isotropic hardening is assumed, while the tangent modulus is set –as a best practice - to a very small non-zero value (can still be considered perfectly plastic behaviour) to avoid numerical instability.
As a best practice, symmetry conditions are exploited to avoid using excessive amount of elements in the model. Here this simplifies to a quarter model, as its assumed that both dies are moving towards each other by 0.5 mm. Note that if the bottom die would be fixed, only the vertical symmetry could be utilized, i.e. A half-model would be required.

## Slide 8: Numerical Analysis – From Physical Problem to Final Product
Physical Problem
Numerical Model
Physical Prototype
Final Product
Physical Principles
System of Algebraic Equations
Governing equations
Boundary conditions
FEA approximate
Stiffness matrix
Nodal vector (disp.)
Force vector
Solid Mechanics
User Inputs
Pre-Processing
CAD Model
Material Properties
Load Case
Forging
Assumptions
Hand Calculations
Experimental Data
Outputs
Post-Processing
Evaluation of outputs/state variables
Validation and verification of results against hand calculations and experiments
Notes: Numerical Analysis – From Physical Problem to Final Product
In a simulation driven design approach, engineers go from from physical problem to protype and then final product through a numerical model, i.e. a FEA simulation.
In is pivotal for engineers to fully understand the problem at hand as the model requires in the pre-processing stage some user inputs such as
  CAD Model
  Material Properties
  Load Case
Next the physical principles describingng need to be defined, meaning
  Governing equations describing the physics in the form of partial differential equations (PDEs)
  The Boundary conditions derived from the relevant load cases
  Any assumptions and/or simplification that are made to describe the problem
  It must be noted that besides the numerical analysis, solving these engineering problems cis also done analytically (hand calculation for simple problems) or experimentally (empirical data which often inform numerical models, e.g. Constitutive behaviours).
If we take solid mechanics problem like forging for instance, the main system of algebraic equation that is being solved for a static structural analysis is the approximation of the nodal displacement based on its relationship with the applied force and the stiffness matrix K.
  This yields the outputs in the form of state variables, commonly displayed in colourful images, highlighting the distribution of e.g. the elemental displacements and stresses
  Another common post-processing step is to validate the FEA (best practices and e.g. mesh quality) and if possible verify it against hand calculations and experimental data

## Slide 9: Numerical Analysis – Matrix Formulation in FEA
Physical Problem
Numerical Model
Physical Prototype
Final Product
Physical Principles
System of Algebraic Equations
Governing equations
Boundary conditions
FEA approximate
Strong Form
Assumptions
Weak Form
E.g.: PDEs. + BCs for linear Elasticity (Translational equilibrium)
* is the gradient operator, σ is the stress tensor, b is a vector with body forces
꙳ This is obtained by multiplying the strict form with a vector of a test function 𝑤 and integration of the product of strong form and test functions.
*
reduces differentiability requirements,
allows discontinuous derivatives (e.g., at element boundaries),
is directly compatible with finite element basis functions.
Discrete Form
Substituting shape functions into the weak form and performing the integrals gives the element stiffness matrices and element load vectors.
Assembling all element contributions leads to the Matrix Formulation:
Integration
꙳
PDE
BC
Notes: Numerical Analysis – Matrix Method in FEA
Discrete Form or Matrix Formulation in FEA — Brief Explanation
  In Finite Element Analysis, the Matrix Method refers to expressing the governing equations of a physical system in algebraic matrix form, typically:
    where
    K = global stiffness matrix (assembled from element matrices),
    u = vector of unknown nodal degrees of freedom (displacements, temperatures, etc.),
    f = global force/load vector.
  This matrix system is what the computer ultimately solves. The Matrix Method is not a separate theory; rather, it is the computational embodiment of the finite element discretization.
How It Connects to the Strong and Weak Forms
  The strong form is the original differential equation plus boundary conditions — e.g., for linear elasticity:
  The strong form requires:
  pointwise satisfaction of the differential equation,
  differentiability conditions that are often too strict for piecewise-polynomial finite elements.
  To allow approximate solutions, we convert the strong form to a weak form by:
    multiplying by a test (weight) function,
    integrating over the domain,
    applying integration by parts.
  This yields something like:
  The weak form:
    reduces differentiability requirements,
    allows discontinuous derivatives (e.g., at element boundaries),
    is directly compatible with finite element basis functions.
Discretization → Matrix Form
  The final step is representing the unknown function and weight functions using finite element shape functions:
  Substituting shape functions into the weak form and performing the integrals gives the element stiffness matrices and element load vectors.
  Assembling all element contributions leads to the Matrix Formulation:
Numerical Analysis – Matrix Method in FEA
Discrete Form or Matrix Formulation in FEA — Brief Explanation
  In Finite Element Analysis, the Matrix Method refers to expressing the governing equations of a physical system in algebraic matrix form, typically: 𝐊𝐮=𝐟
    where
    K = global stiffness matrix (assembled from element matrices),
    u = vector of unknown nodal degrees of freedom (displacements, temperatures, etc.),
    f = global force/load vector.
  This matrix system is what the computer ultimately solves. The Matrix Method is not a separate theory; rather, it is the computational embodiment of the finite element discretization.
How It Connects to the Strong and Weak Forms
  The strong form is the original differential equation plus boundary conditions — e.g., for linear elasticity: ∇⋅𝜎+𝑏=0
  The strong form requires:
  pointwise satisfaction of the differential equation,
  differentiability conditions that are often too strict for piecewise-polynomial finite elements.
  To allow approximate solutions, we convert the strong form to a weak form by:
    multiplying by a test (weight) function,
    integrating over the domain,
    applying integration by parts.
  This yields something like: ∫_Ω▒〖𝑤∗("∇⋅σ" )〗 𝑑Ω=∫_Ω▒〖𝑤∗𝑏〗 𝑑Ω
  The weak form:
    reduces differentiability requirements,
    allows discontinuous derivatives (e.g., at element boundaries),
    is directly compatible with finite element basis functions.
Discretization → Matrix Form
  The final step is representing the unknown function 𝑢and weight functions 𝑣using finite element shape functions: 𝑢≈𝑁(𝑥)" " 𝐮
  Substituting shape functions into the weak form and performing the integrals gives the element stiffness matrices and element load vectors.
  Assembling all element contributions leads to the Matrix Formulation: 𝐊𝐮=𝐟

## Slide 10: Governing Equations Linear Case
1. Start with the equilibrium equation in 1D:
  Represents force equilibrium in the x-direction
  ​ is the body force per unit length
2. Constitutive relation (Hooke’s law):
  Stress is proportional to strain via Young’s modulus 𝑬
3. Strain-displacement relation:
  Strain is the derivative of displacement
4. Combine to get the governing differential equation:
  This is the strong form of the equilibrium equation
1D
2D
1. Start from the generalized equilibrium equation:
  is the transpose of the strain-displacement operator, acting on the stress vector.
  represents body forces.
2. Displacement vector and strain-disp. relation:
3. Stress-strain relation (Hooke’s law for plane strain):
  [D]: Material stiffness matrix (depends on E and ν)
  ν: Poisson’s ratio (lateral strain/axial strain)”.
4. Weak form for FEM:
Notes: Governing Equations Linear Case
Context:
This slide introduces the governing equations for a linear case in FEA using the Matrix Formulation.
It shows the transition from 1D differential form to 2D matrix form, which is the foundation for FEM formulations.
Derivation Notes:
In many introductory FEM derivations (like this slide), body forces are ignored to simplify the formulation and focus on stress-strain relationships and stiffness matrix assembly.
Complementary Notes:
a) Explain the jump from 1D to 2D:
In 1D: .
In 2D plane strain: stresses and strains become vectors, and material properties become a matrix.
b) Discuss the stiffness matrix [D]:
Derived from generalized Hooke’s law for isotropic materials.
Depends on Young’s modulus (E) and Poisson’s ratio ().
c) Highlight why plane strain assumption matters:
, so out-of-plane strain is negligible.
Common in forging and rolling processes where thickness is constrained.
Governing Equations Linear Case
Context:
This slide introduces the governing equations for a linear case in FEA using the Matrix Formulation.
It shows the transition from 1D differential form to 2D matrix form, which is the foundation for FEM formulations.
Derivation Notes:
In many introductory FEM derivations (like this slide), body forces are ignored to simplify the formulation and focus on stress-strain relationships and stiffness matrix assembly.
Complementary Notes:
a) Explain the jump from 1D to 2D:
In 1D: 𝜎_𝑥𝑥=𝐸𝜀_𝑥𝑥.
In 2D plane strain: stresses and strains become vectors, and material properties become a matrix.
b) Discuss the stiffness matrix [D]:
Derived from generalized Hooke’s law for isotropic materials.
Depends on Young’s modulus (E) and Poisson’s ratio (𝜈).
c) Highlight why plane strain assumption matters:
𝜀_𝑧≈0, so out-of-plane strain is negligible.
Common in forging and rolling processes where thickness is constrained.

## Slide 11: Plane Stress vs Plane Strain Hooke’s Law
Plane Stress
Assumes (thin plates, negligible out-of-plane stress).
Stresses:
Strains:
Plane Strain
Assumes (long/thick bodies, constrained in z-direction).
Stresses:
Strains:
Notes: Plane Stress vs Plane Strain Hooke’s Law
Explain physical meaning:
Plane Stress → thin structures (e.g., sheet metal).
Plane Strain → thick or long structures (e.g., dams, tunnels).
Emphasize difference in assumptions:
Plane Stress neglects out-of-plane stress.
Plane Strain neglects out-of-plane strain.
Show how Hooke’s law adapts for each case.
Mention impact on stiffness: Plane Strain is effectively stiffer because of constraint in z-direction.

## Slide 12: Forging in Plane Strain with Coulomb Friction (1/2)
Problem Setup
  Strip half-width = 𝑎
  Thickness = ℎ
  Coordinate 𝑥
  measured from centerline (0 → a)
  Rigid flat dies
  Coulomb friction at die/workpiece interface
  Examination of a thin vertical slab of width .
Assumptions (1/2)
  Geometry & Kinematics
    Plane strain: =0 ​
    Width in z-direction ≫ thickness
    No barreling
    Uniform thickness ℎ
    Symmetry at 𝑥=0
  Material
    Rigid-perfectly plastic
    Isotropic
    Constant flow stress
Assumptions (2/2)
  Friction
    Coulomb friction:𝜏=𝜇𝑃τ
    Constant coefficient 𝜇
  Stress State
    Normal pressure from dies: 𝑃(𝑥)
    Longitudinal stress in strip: (𝑥)
    Plane strain condition governs yield
Notes: Forging in Plane Strain with Coulomb Friction (1/2)
Physical Problem Setup
We analyze compression of a long strip between rigid flat dies.
Because the strip is very long in the out-of-plane direction, deformation in that direction is constrained — giving plane strain conditions.
We study only half the strip due to symmetry.
The goal is to determine how the contact pressure varies from the free edge to the centerline.
Why Pressure Is Not Uniform?
If friction were zero, pressure would be uniform.
But friction resists outward flow. To overcome this resistance, the internal compressive stress must increase toward the center.
That is why pressure becomes non-uniform and exponential. (Note: There is a Quiz question on this on the next slide).
Key Modeling Assumptions
These assumptions are critical:
Plane strain means the strip is very wide and cannot deform out of plane.
Rigid-perfectly plastic means:
  No elastic deformation
  No strain hardening
  Yield stress is constant
Coulomb friction means shear stress is proportional to local pressure.
These assumptions allow a closed-form analytical solution.

## Slide 13: Forging in Plane Strain with Coulomb Friction (2/2)
Integration on both sides
Considering that the longitudinal stress is zero at a free surface (), the integration of with and yields
Equilibrium forces in x-direction
Distortion-Energy Criterion
Diffrintiation and Substitution
Assuming Coulomb’s law of sliding friction, substituting into the above equation and rearranging
Source: G.E. Dieter“Mechanical Metallurgy”, 3rd ed., McGraw-Hill, 1986
Differential equation for open-die forging of constant-thickness plates considering plane strain conditions
Quiz Question: How does the pressure distribution change from the centre to the free surface?
Notes: Forging in Plane Strain with Coulomb Friction (2/2)
This slide summarizes how the differential equation for open-die forging of constant-thickness plates considering plane strain conditions is derived according to G.E. Dieter“Mechanical Metallurgy”, 3rd ed., McGraw-Hill, 1986.
Note: Please refer to the schematic drawing on the above slide for context regarding the variables used.
Quiz Question Answer:
The pressure distribution decreases from the centre towards the free edge. The trendline is exponential.

## Slide 14: Boundary Conditions Forging & Numerical Solution
Discretization
y
x
Boundary Conditions
Symmetry Conditions: Zero displacement and shear stress
Discretization/Meshing: Divide domain into elements and nodes
Problem reduction: Determining displacement values only at nodes
Shape functions: Use linear or polynomial interpolation to relate displacement within an element to nodal values
Notes: Boundary Conditions Forging & Numerical Solution
The problem is simplified to a 2D quarter model, requiring symmetry boundary conditions at the edges limiting the normal displacements and shear forces to zero, while a displacement load of -1 mm is applied in negative y-direction.
The geometry is meshed with Quad4 (linear interpolation) elements with matching nodes between die and workpiece (ensured though an applied shared topology).
The problem is reduced by determining the displacement only at the nodes and interpolating the displacement within the element through the shape functions.
Note: In reference to the top-right image, the shear stress is zero only when considering case 1, i.e. frictionless contact.

## Slide 15: How to Find Nodal Displacements?
Mathematical Model (Boundary Value Problem)
System of algebraic equations in nodal displacements*
Nodal displacements
&
Post-Processing
Invert
Element-by-element interpolation for displacements
* Notes: Each algebraic equation will relate a nodal displacement to its neighbors.
Notes: How to Find Nodal Displacements?
0 .Big Concept to Emphasize
The entire finite element method can be summarized as:
Approximate displacement field
Convert differential equations into algebraic equations
Solve for nodal displacements
Recover stresses and strains
Everything revolves around nodal displacements.
 The finite element method does not directly solve for stresses. It solves for nodal displacements, and all other field quantities are derived from them.
1. Mathematical Model (Boundary Value Problem)
We start with the continuum mechanics formulation of the problem.
This means we define:
Equilibrium equations
Constitutive law (e.g., linear elasticity or plasticity)
Strain–displacement relations
Boundary conditions
Together, these form a boundary value problem (BVP).
However, solving the exact differential equations for complex geometries is usually impossible analytically.
So we discretize the domain into finite elements.
Inside each element, we approximate the displacement field using interpolation functions, also called shape functions.
For a 4-node quadrilateral element:
So instead of solving for continuous displacement fields, we solve for nodal displacement values.
2. System of Algebraic Equations in Nodal Displacements
Once we insert the interpolated displacements into:
The weak form of equilibrium or
The principle of virtual work
we obtain a matrix equation:
  Where:
    = global stiffness matrix
    = vector of unknown nodal displacements
    = external force vector
Each row of this system corresponds to force equilibrium at a node.
Each equation relates a nodal displacement to its neighboring nodes.
This happens because elements share nodes — so their stiffness contributions assemble into a global system.
That’s why FEA becomes a large coupled algebraic system.
3. Nodal Displacements
After applying boundary conditions and solving the matrix system, we obtain the primary unknowns:
These are the nodal displacements in each direction.
Important concept:
In displacement-based finite element methods, nodal displacements are the only primary unknowns.
Everything else — strain, stress, reaction forces — is derived from them.
At this stage, we know how every node in the mesh has moved.
4. Post-Processing - and
Now we reconstruct continuous field quantities inside each element.
Using the same shape functions:
Strains are obtained from spatial derivatives:
And stresses follow from the constitutive law:
So the workflow is:
  Nodal displacements → Strains → Stresses
  This step is called post-processing.
It allows us to visualize:
  Deformation contours
  Stress distributions
  Reaction forces
But remember: stresses are secondary quantities — derived from nodal displacements.
4-Node Linear Element
This element has:
4 nodes
2 DOFs per node (in 2D)
Linear shape functions
That means:
  Displacement varies linearly inside the element
  Strain is constant within the element
  This is why coarse meshes can produce piecewise-constant stress patterns.
How to Find Nodal Displacements?
0 .Big Concept to Emphasize
The entire finite element method can be summarized as:
Approximate displacement field
Convert differential equations into algebraic equations
Solve for nodal displacements
Recover stresses and strains
Everything revolves around nodal displacements.
 The finite element method does not directly solve for stresses. It solves for nodal displacements, and all other field quantities are derived from them.
1. Mathematical Model (Boundary Value Problem)
We start with the continuum mechanics formulation of the problem.
This means we define:
Equilibrium equations
Constitutive law (e.g., linear elasticity or plasticity)
Strain–displacement relations
Boundary conditions
Together, these form a boundary value problem (BVP).
However, solving the exact differential equations for complex geometries is usually impossible analytically.
So we discretize the domain into finite elements.
Inside each element, we approximate the displacement field using interpolation functions, also called shape functions.
For a 4-node quadrilateral element:
  𝑢(𝑥ⓜ,𝑦)=∑128_(𝑖=1)^4▒𝑁_𝑖 (𝑥ⓜ,𝑦)" " 𝑢_𝑖
  𝑣(𝑥ⓜ,𝑦)=∑128_(𝑖=1)^4▒𝑁_𝑖 (𝑥ⓜ,𝑦)" " 𝑣_𝑖
So instead of solving for continuous displacement fields, we solve for nodal displacement values.
2. System of Algebraic Equations in Nodal Displacements
Once we insert the interpolated displacements into:
The weak form of equilibrium or
The principle of virtual work
we obtain a matrix equation:
  𝐊𝐮=𝐟
  Where:
    𝐊= global stiffness matrix
    𝐮= vector of unknown nodal displacements
    𝐟= external force vector
Each row of this system corresponds to force equilibrium at a node.
Each equation relates a nodal displacement to its neighboring nodes.
This happens because elements share nodes — so their stiffness contributions assemble into a global system.
That’s why FEA becomes a large coupled algebraic system.
3. Nodal Displacements 𝑢_(𝑥_𝑖 ),𝑢_(𝑦_𝑖 )
After applying boundary conditions and solving the matrix system, we obtain the primary unknowns:
  𝑢_(𝑥_𝑖 ), 𝑢_(𝑦_𝑖 )
These are the nodal displacements in each direction.
Important concept:
In displacement-based finite element methods, nodal displacements are the only primary unknowns.
Everything else — strain, stress, reaction forces — is derived from them.
At this stage, we know how every node in the mesh has moved.
4. Post-Processing - 𝑢_𝑦 (𝑥ⓜ,𝑦)and 𝜎_𝑦𝑦 (𝑥ⓜ,𝑦)
Now we reconstruct continuous field quantities inside each element.
Using the same shape functions:
  𝑢_𝑦 (𝑥ⓜ,𝑦)=∑128▒𝑁_𝑖 (𝑥ⓜ,𝑦)" " 𝑢_(𝑦_𝑖 )
Strains are obtained from spatial derivatives:
  𝜀=𝐁𝐮
And stresses follow from the constitutive law:
  𝜎=𝐃𝜀
So the workflow is:
  Nodal displacements → Strains → Stresses
  This step is called post-processing.
It allows us to visualize:
  Deformation contours
  Stress distributions
  Reaction forces
But remember: stresses are secondary quantities — derived from nodal displacements.
4-Node Linear Element
This element has:
4 nodes
2 DOFs per node (in 2D)
Linear shape functions
That means:
  Displacement varies linearly inside the element
  Strain is constant within the element
  This is why coarse meshes can produce piecewise-constant stress patterns.

## Slide 16
Simulation in Ansys Mechanical software and Comparison with Analytical Calculation
Plain Strain Forging
Notes: Simulation in Ansys MechanicalTM and Comparison with Analytical (Hand) Calculation - Plain Strain Forging
The following tutorial will walk you through the simulation setup in Ansys Mechanical, covering both the frictionless as well as friction case and comparing the numerical with the analytical results.

## Slide 17: Ansys Forging Tutorial Case 1 (1/8) – Pre-Process
Open the project file in Ansys WorkbenchTM: Forging_Tutorial_Start.wbpz
Review the Engineering Data in cell A2 of the Static Structural analysis system.
Review the Geometry in Ansys DiscoveryTM in cell A3 of the Static Structural analysis system, which is a shell CAD model. Notice that the A3 properties specify a 2D analysis*.
1
3
Top die
Workpiece
2
* Notes: By setting the Analysis Type to 2D, we apply the Governing Equations discussed in Slide 9/10.
Notes: Ansys Forging Tutorial Case 1 (1/8) – Pre-Process
Open the project file in Ansys WorkbenchTM: Forging_Tutorial_Start.wbpz
Review the Engineering Data in cell A2 of the Static Structural analysis system.
Review the Geometry in Ansys DiscoveryTM in cell A3 of the Static Structural analysis system, which is a shell CAD model. Notice that the A3 properties specify a 2D analysis.
  Note: By setting the Analysis Type to 2D, we apply the Governing Equations discussed in Slide 9.

## Slide 18: Ansys Forging Tutorial Case 1 (2/8) – Pre-Process
Open Ansys MechanicalTM by editing cell A4 and then expand the Geometry in the project tree.
Assign the right material properties to the die and workpiece.
In the details window of the Geometry, set the 2D Behaviour to Plane Strain*.
2
1
3
* Notes: 2D Hooke’s Law of plane strain (recall Slide 9), where out-of-plane strain is zero, preventing deformation in the thickness direction.
Notes: Ansys Forging Tutorial Case 1 (2/8) – Pre-Process
Open Ansys MechanicalTM by editing cell A4 and then expand the Geometry in the project tree.
Assign the right material properties to the die and workpiece.
In the details window of the Geometry, set the 2D Behaviour to Plane Strain
  Note: Recall Slide 9 to utilize the plane strain definition of the Hooke’s Law

## Slide 19: Ansys Forging Tutorial Case 1 (3/8) – Pre-Process
Review the contacts between the workpiece and die, which by default are set to bonded. Change this to Frictional and set it for case 1, i.e. (Alternatively it can also be set to Frictionless for case 1). Ensure that the contact and target edges are correctly scoped*.
1
1
* Note: In rigid-to-flexible contact pairs—including cases where a body is made very stiff to approximate rigidity—the rigid (or very stiff) body's surface must always be scoped as the target, and the flexible/deformable body's surface as contact (slave).
Notes: Ansys Forging Tutorial Case 1 (3/8) – Pre-Process
Review the contacts between the workpiece and die, which by default are set to bonded. Change this to frictional and set it for case 1, i.e. .
  Note: In rigid-to-flexible contact pairs—including cases where a body is made very stiff to approximate rigidity—the rigid (or very stiff) body's surface must always be scoped as the target, and the flexible/deformable body's surface as contact (slave).
Ansys Forging Tutorial Case 1 (3/8) – Pre-Process
Review the contacts between the workpiece and die, which by default are set to bonded. Change this to frictional and set it for case 1, i.e. 𝜇=0.
  Note: In rigid-to-flexible contact pairs—including cases where a body is made very stiff to approximate rigidity—the rigid (or very stiff) body's surface must always be scoped as the target, and the flexible/deformable body's surface as contact (slave).

## Slide 20: Ansys Forging Tutorial Case 1 (4/8) – Pre-Process
Edit the Mesh and make the following changes*:
  Element Order: Linear
  Element Size: 0.25 mm
Ensure uniform mesh sizing is applied.
* Notes:
Both sides of the contact interface should have comparable mesh density to avoid numerical instability and abrupt contact changes.
It is best practice to refine the mesh sufficiently to obtain mesh-independent results.
Any additional face, edge sizing or mesh methods were intentionally forego but users could apply a courser mesh to the die and a local refinement to the interface to balance accuracy and computational cost.
Linear instead of quadratic elements were utilized as a relative fine mesh was used for the simple frictionless case (quadratic elements will be used for the frictional case).
1
2
1
Notes: Ansys Forging Tutorial Case 1 (4/8) – Pre-Process
Edit the Mesh and make the following changes*:
  Element Order: Linear
  Element Size: 0.25 mm.
Ensure uniform mesh sizing is applied.
  Notes:
Both sides of the contact interface should have comparable mesh density to avoid numerical instability and abrupt contact changes.
It is best practice to refine the mesh sufficiently to obtain mesh-independent results.
Any additional face, edge sizing or mesh methods were intentionally forego but users could apply a courser mesh to the die and a local refinement to the interface to balance accuracy and computational cost.
Linear instead of quadratic elements were utilized as a relative fine mesh was used for the simple frictionless case (quadratic elements will be used for the frictional case).

## Slide 21: Ansys Forging Tutorial Case 1 (5/8) – Pre-Process
Apply displacement constraints according to the symmetry and boundary conditions (recall slide 11):
  Edge on x-axis: mm
  Edges on y-axis: mm
  Top die edge: mm ( due to symmetry)
* Notes: Alternatively, one could use symmetry conditions instead of the displacement constraints.
1
Notes: Ansys Forging Tutorial Case 1 (5/8) – Pre-Process
Apply displacement constraints according to the symmetry and boundary conditions (recall slide 11):
  Edge on x-axis: mm
  Edges on y-axis: mm
  Top die edge: mm ( due to symmetry)
* Notes: Alternatively, one could use symmetry conditions instead of the displacement constraints.
Ansys Forging Tutorial Case 1 (5/8) – Pre-Process
Apply displacement constraints according to the symmetry and boundary conditions (recall slide 11):
  Edge on x-axis: 𝑢_𝑦=0 mm
  Edges on y-axis: 𝑢_𝑥=0 mm
  Top die edge: 𝑢_𝑧=−0,5 mm (𝛿/2 due to symmetry)
* Notes: Alternatively, one could use symmetry conditions instead of the displacement constraints.

## Slide 22: Ansys Forging Tutorial Case 1 (6/8) – Pre-Process
As this is considered a quasi-static case, adjust the strain rate, i.e. the step end time accordingly. A strain rate of is assumed.
Now solve the problem through the Solution in the project tree.
2
1
Notes: Ansys Forging Tutorial Case 1 (6/8) – Pre-Process
As this is considered a quasi-static case, adjust the strain rate, i.e. the step end time accordingly. A strain rate of is assumed.
Now solve the problem through the Solution in the project tree.
Ansys Forging Tutorial Case 1 (6/8) – Pre-Process
As this is considered a quasi-static case, adjust the strain rate, i.e. the step end time accordingly. A strain rate of 10^(−3) 𝑠^(−1) is assumed.
  𝜀=Δ𝐿/𝐿_0 =(1 𝑚𝑚)/(10 𝑚𝑚)=0.1
  𝑡=𝜀/𝜀 ̇ =0.1/10^(−3) =100 𝑠
Now solve the problem through the Solution in the project tree.

## Slide 23: Ansys Forging Tutorial Case 1 (7/8) – Pre-Process
Add a (i) total and (ii) directional deformation and (iii) normal stress solution output.
For the normal stress and directional deformation, specify the y-direction and scope the result only to the workpiece.
Retrieve both results and review them.
1
1
3
2
2
Notes: Ansys Forging Tutorial Case 1 (7/8) – Pre-Process
Add a (i) total and (ii) directional deformation and (iii) normal stress solution output.
For the normal stress and directional deformation, specify the y-direction and scope the result only to the workpiece.
Retrieve both results and review them.

## Slide 24: Ansys Forging Tutorial Case 1 (8/8) – Post-Process
The analytical result of the normal stress in y-direction along the x-axis – assuming frictionless contact – is 461.88 MPa (constant) which is matches with the numerical (FEA) result.
Analytical solution for case 1 with =0:
0
Notes: Ansys Forging Tutorial Case 1 (8/8) – Post-Process
The analytical result of the normal stress in y-direction along the x-axis – assuming frictionless contact – is 461.88 MPa (constant) which is matches with the numerical (FEA) result.
Analytical solution for case 1 with =0:
  Substituting the values (see problem statement) yields an exact match with FEA.
Ansys Forging Tutorial Case 1 (8/8) – Post-Process
The analytical result of the normal stress in y-direction along the x-axis – assuming frictionless contact – is 461.88 MPa (constant) which is matches with the numerical (FEA) result.
Analytical solution for case 1 with 𝜇=0:
  Substituting the values (see problem statement) yields an exact match with FEA.

## Slide 25: Ansys Forging Tutorial Case 2 (1/9) – Pre-Process
For case 2 set the friction coefficient to =0.1
  Note that this introduces contact non-linearity in addition to the material non-nonlinearity (perfectly plastic).
  This in turn causes higher distortion of elements and increases the likelihood of convergence problems due to highly distorted and inverted elements. As a consequence, the following settings must be applied.
Set the contact behaviour to asymmetric and the formulation to Augmented Lagrange*
Use quadratic instead of linear elements. *1
* Notes:
Asymmetric contact behaviour can have significant effects on convergence, mesh distortion, and stick-slip phenomena, especially in simulations involving nonlinear contact and material nonlinearity.
In cases of severe mesh distortion, the Augmented Lagrange remains more robust than e.g. penalty-only approaches and accurately captures stick-slip transitions and frictional sliding due to its iterative enforcement of contact constraints, reducing the likelihood of artificial slip or sticking compared to penalty-only methods
*1 Notes:
Quadratic elements can improve solution accuracy for nonlinear contact and material nonlinearity due to their ability to represent nonlinear displacement fields more effectively.
They handle bending and shear energy much better than linear elements, reducing locking and excessive stiffness, especially in distorted meshes or regions with high gradients
1
2
3
2
Notes: Ansys Forging Tutorial Case 2 (1/9) – Pre-Process
For case 2 set the friction coefficient to =0.1
  Note that this introduces contact non-linearity in addition to the material non-nonlinearity (perfectly plastic).
  This in turn causes higher distortion of elements and increases the likelihood of convergence problems due to highly distorted and inverted elements. As a consequence, the following settings must be applied.
Set the contact behaviour to asymmetric and the formulation to Augmented Lagrange*
Use quadratic instead of linear elements. *1
* Notes:
Asymmetric contact behaviour can have significant effects on convergence, mesh distortion, and stick-slip phenomena, especially in simulations involving nonlinear contact and material nonlinearity.
In cases of severe mesh distortion, the Augmented Lagrange remains more robust than e.g. penalty-only approaches and accurately captures stick-slip transitions and frictional sliding due to its iterative enforcement of contact constraints, reducing the likelihood of artificial slip or sticking compared to penalty-only methods
*1 Notes:
Quadratic elements can improve solution accuracy for nonlinear contact and material nonlinearity due to their ability to represent nonlinear displacement fields more effectively.
They handle bending and shear energy much better than linear elements, reducing locking and excessive stiffness, especially in distorted meshes or regions with high gradients
Ansys Forging Tutorial Case 2 (1/9) – Pre-Process
For case 2 set the friction coefficient to 𝜇=0.1
  Note that this introduces contact non-linearity in addition to the material non-nonlinearity (perfectly plastic).
  This in turn causes higher distortion of elements and increases the likelihood of convergence problems due to highly distorted and inverted elements. As a consequence, the following settings must be applied.
Set the contact behaviour to asymmetric and the formulation to Augmented Lagrange*
Use quadratic instead of linear elements. *1
* Notes:
Asymmetric contact behaviour can have significant effects on convergence, mesh distortion, and stick-slip phenomena, especially in simulations involving nonlinear contact and material nonlinearity.
In cases of severe mesh distortion, the Augmented Lagrange remains more robust than e.g. penalty-only approaches and accurately captures stick-slip transitions and frictional sliding due to its iterative enforcement of contact constraints, reducing the likelihood of artificial slip or sticking compared to penalty-only methods
*1 Notes:
Quadratic elements can improve solution accuracy for nonlinear contact and material nonlinearity due to their ability to represent nonlinear displacement fields more effectively.
They handle bending and shear energy much better than linear elements, reducing locking and excessive stiffness, especially in distorted meshes or regions with high gradients

## Slide 26: Ansys Forging Tutorial Case 2 (2/9) – Pre-Process
* Notes:
Always turn on large deflections for nonlinear contact problems to ensure the solver can handle geometric nonlinearity. For Coupled Field, Static Structural, and Transient Structural analyses, this property determines whether the solver should take into account large deformation effects such as large deflection, large rotation, and large strain. Set Large Deflection to On if you expect large deflections (as in the case of a long, slender bar under bending) or large strains (as in a metal-forming problem). See documentation for details: 16.1.3. Solver Controls
*1 Notes:
For models with severe nonlinearities (e.g., high friction, large deformations, or stick-slip), using the unsymmetric Newton-Raphson option can improve convergence. This is particularly helpful when friction coefficients are high or when parts of the model undergo severe distortion.
Proceed to the Analysis Settings of the Static Structural analysis system and enable Large Deflection Setting.*
Also set the Newton-Raphson Option to unsymmetric. This property allows you to specify how often the stiffness matrix is updated during the solution process.
1
2
1
Notes: Ansys Forging Tutorial Case 2 (2/9) – Pre-Process
Proceed to the Analysis Settings of the Static Structural analysis system and enable Large Deflection Setting.*
Also set the Newton-Raphson Option to unsymmetric. This property allows you to specify how often the stiffness matrix is updated during the solution process.
* Notes:
Always turn on large deflections for nonlinear contact problems to ensure the solver can handle geometric nonlinearity. For Coupled Field, Static Structural, and Transient Structural analyses, this property determines whether the solver should take into account large deformation effects such as large deflection, large rotation, and large strain. Set Large Deflection to On if you expect large deflections (as in the case of a long, slender bar under bending) or large strains (as in a metal-forming problem). See documentation for details: 16.1.3. Solver Controls
*1 Notes:
For models with severe nonlinearities (e.g., high friction, large deformations, or stick-slip), using the unsymmetric Newton-Raphson option can improve convergence. This is particularly helpful when friction coefficients are high or when parts of the model undergo severe distortion.

## Slide 27: Ansys Forging Tutorial Case 2 (3/9) – Pre-Process
In order to obtain the pressure distribution on the bottom edge (along the x-axis) of the workpiece insert a construction path in the model and define the end of the x coordinate at 50 mm (referring to the global coordinate system).
In the solution section of the project tree duplicate the normal stress solution in y-direction (RMB).
Scope the normal stress in y direction to the path and solve the static structural problem.
1
2
3
Notes: Ansys Forging Tutorial Case 2 (3/9) – Pre-Process
In order to obtain the pressure distribution on the bottom edge (along the x-axis) of the workpiece insert a construction path in the model and define the end of the x coordinate at 50 mm (referring to the global coordinate system).
In the solution section of the project tree duplicate the normal stress solution in y-direction (RMB).
Scope the normal stress in y direction to the path and solve the static structural problem.

## Slide 28: Ansys Forging Tutorial Case 2 (4/9) – Post-Process
Shown here are the total and directional deformations in x- and y-axis.
If you animate the deformation over time one can observe that the is uniform at the beginning and then transitioning into a zig-zag pattern that initially alternates and then settles into a state in which is caused by a stick-slip behaviour at the contact.
Barreling is a three-dimensional effect caused by differential radial flow. Plane strain enforces zero out-of-plane strain, which suppresses the kinematics necessary for classical barreling. Instead, deformation localizes near the die-contact corners due to frictional shear and geometric constraints.
Notes: Ansys Forging Tutorial Case 2 (4/9) – Post-Process
Shown here are the total and directional deformations in x- and y-axis.
If you animate the deformation over time one can observe that the is uniform at the beginning and then transitioning into a zig-zag pattern that initially alternates and then settles into a state in which is caused by a stick-slip behaviour at the contact.
Barreling is a three-dimensional effect caused by differential radial flow. Plane strain enforces zero out-of-plane strain, which suppresses the kinematics necessary for classical barreling. Instead, deformation localizes near the die-contact corners due to frictional shear and geometric constraints.

## Slide 29: Ansys Forging Tutorial Case 2 (5/9) – Post-Process
Shown on the right are the normal stresses in y-direction across the workpiece and along the bottom (centreline) edge.
The graph shows a stepped pressure distribution with only minor deviation at x = 0mm and x = 50mm.
Notes: Ansys Forging Tutorial Case 2 (5/9) – Post-Process
Shown on the right are the normal stresses in y-direction across the workpiece and along the bottom (centreline) edge.
The graph shows a stepped pressure distribution with only minor deviation at x = 0mm and x = 50mm.

## Slide 30: Ansys Forging Tutorial Case 2 (6/9) – Post-Process
Shown here are the normal stresses in y-direction across the workpiece and along the bottom (centreline) edge for the frictionless and friction case compared with the analytical results.
The frictionless case shows a perfect match while the frictional case displayed a stepped rather than exponential trendline. However, the values at the symmetry and free edge and the intermediate sample points vary only slightly around the analytical values. A curve fit of the FEA results would yield a close correlation with the hand calculation.
Notes: Ansys Forging Tutorial Case 2 (6/9) – Post-Process
Shown here are the normal stresses in y-direction across the workpiece and along the bottom (centreline) edge for the frictionless and friction case compared with the analytical results.
The frictionless case shows a perfect match while the frictional case displayed a stepped rather than exponential trendline. However, the values at the symmetry and free edge and the intermediate sample points vary only slightly around the analytical values. A curve fit of the FEA results would yield a close correlation with the hand calculation.

## Slide 31: Ansys Forging Tutorial Case 2 (7/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Assumptions of analytical result
  Constant thickness h
  Small deformation
  Rigid-perfectly plastic material
  Constant flow stress σ_0
  Constant friction coefficient
  No change in contact length
  No geometry update
Note:
At the beginning of deformation, these assumptions are approximately true.
When changing the display time to a small value (here 1 sec) the FEA matches the exponential shape.
Notes: Ansys Forging Tutorial Case 2 (7/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Assumptions of Analytical result
  Constant thickness h
  Small deformation
  Rigid-perfectly plastic material
  Constant flow stress σ_0
  Constant friction coefficient
  No change in contact length
  No geometry update
 NOTE: At the beginning of deformation, these assumptions are approximately true, i.e. If you changes the display time to a small value (here we set it to 1 sec), you can identify the exponential normal stress distribution.

## Slide 32: Ansys Forging Tutorial Case 2 (8/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Changing Geometry (Large Deformation)
  In the FEA:
    Thickness decreases
    Contact length changes
    Surfaces rotate slightly
    Local curvature may develop
    But the analytical solution assumes constant .
    Since the exponent contains:
    as decreases, the pressure gradient steepens non-uniformly.
    This destroys the clean exponential form.
Strain Hardening
  If your material is elastic-plastic with hardening:
  Now flow stress increases toward the centre (where strain is largest).
  So pressure becomes:
  This makes the pressure profile no longer purely exponential.
  Often this produces plateau-like or stepped regions.
Notes: Ansys Forging Tutorial Case 2 (8/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Changing Geometry (Large Deformation)
  In the FEA:
    Thickness decreases
    Contact length changes
    Surfaces rotate slightly
    Local curvature may develop
    But the analytical solution assumes constant .
    Since the exponent contains:
    as decreases, the pressure gradient steepens non-uniformly.
    This destroys the clean exponential form.
Strain Hardening
  If your material is elastic-plastic with hardening:
  Now flow stress increases toward the center (where strain is largest).
  So pressure becomes:
  This makes the pressure profile no longer purely exponential.
  Often this produces plateau-like or stepped regions.
Ansys Forging Tutorial Case 2 (8/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Changing Geometry (Large Deformation)
  In the FEA:
    Thickness ℎ decreases
    Contact length changes
    Surfaces rotate slightly
    Local curvature may develop
    But the analytical solution assumes constant ℎ.
    Since the exponent contains: 2𝜇/ℎ
    as ℎ decreases, the pressure gradient steepens non-uniformly.
    This destroys the clean exponential form.
Strain Hardening
  If your material is elastic-plastic with hardening: 𝜎_0→𝜎(𝜀_𝑝 )
  Now flow stress increases toward the center (where strain is largest).
  So pressure becomes: 𝑃(𝑥)∝𝜎(𝜀_𝑝 (𝑥))
  This makes the pressure profile no longer purely exponential.
  Often this produces plateau-like or stepped regions.

## Slide 33: Ansys Forging Tutorial Case 2 (9/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Transition Between Sticking and Sliding
  The analytical solution assumes:
  (sliding everywhere)
  But in real forming at high compression:
  Center region may stick
  Outer region may slide
  So friction law changes locally:
    Sliding:
    Sticking:
  This creates zones with different governing equations, giving piecewise behaviour.
  This is a physically meaningful reason for stepped pressure.
Note:
If you add a contact tool to the solution and observe the status over time you will notice that for the majority of the loading the above split between sticking and sliding.
This non-uniform contact condition in turn contributes to an non-uniform (unlike the frictionless case) deformation pattern.
Notes: Ansys Forging Tutorial Case 2 (9/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Transition Between Sticking and Sliding
  The analytical solution assumes: (sliding everywhere)
  But in real forming at high compression:
  Center region may stick
  Outer region may slide
  So friction law changes locally:
    Sliding:
    Sticking:
  This creates zones with different governing equations, giving piecewise behavior.
  This is a physically meaningful reason for stepped pressure.
Ansys Forging Tutorial Case 2 (9/9) – Post-Process
What causes the differences in the frictional case between the numerical and analytical result?
Transition Between Sticking and Sliding
  The analytical solution assumes: 𝜏=𝜇𝑃 (sliding everywhere)
  But in real forming at high compression:
  Center region may stick
  Outer region may slide
  So friction law changes locally:
    Sliding: 𝜏=𝜇𝑃
    Sticking: 𝜏<𝜇𝑃
  This creates zones with different governing equations, giving piecewise behavior.
  This is a physically meaningful reason for stepped pressure.

## Slide 34: Ansys Education Resources Feedback Survey
Here at Ansys, we rely on your feedback to ensure the educational content we create is up-to-date and fits your teaching needs.
Please click the link below to fill out a short survey (~7 minutes) to help us continue to support academics around the world utilizing Ansys tools in the classroom.
Feedback Survey Link
Notes: Ansys Education Resources Feedback Survey
Feedback Survey link for copy-paste method  https://ansys.typeform.com/to/jcattJI5